## Slide 1: Laboratory Procedures for Complete Dentures

## Slide 2: Laboratory Procedures for Complete Dentures
Primary Cast
Custom Tray Fabrication
Beading/Boxing of Secondary Impression
Master Cast
Denture Base Fabrication
Occlusal Rim Fabrication
Articulation
Teeth Setup
Investing the trial dentures
Curing
Trimming/Finishing and Polishing

## Slide 3: Denture Processing
Steps
Investing
Dewaxing
Packing of acrylic resin
Curing
Devesting
Trimming
Finishing
Polishing

## Slide 4: Sealing
Sealing of cast with wax to prevent plaster from getting under the base

## Slide 5: Investing

## Slide 10: Dewaxing

## Slide 11: Dewaxing

## Slide 12: Dewaxing

## Slide 13: Application of Separating Media
Tin foil
Cellulose lacquers
Solution of alginated compounds
Calcium oleate
Soft soaps
Sodium silicate
Starches
Most commonly used separating medium is sodium alginate solution which is also called as cold mould seal

## Slide 14: Packing

## Slide 15: Remove excess flash

## Slide 16: Curing of Dentures
Short Curing Cycle
Processing at 74ºC for 2 hours with terminal boil at 100ºC for one hour
Long Curing Cycle
Processing at 74ºC for 8 hours with no terminal boil
Processing at 74ºC for 8 hours with terminal boil at 100ºC

## Slide 17: Deflasking & retrieval

## Slide 18: LAB REMOUNT PROCEDURE
Remount the denture with cast on articulator using original plaster index attached with mounting rings of articulator.
Programme articulator in centric relation position
Verify the contact of incisal pin with incisal guide table.

## Slide 19
Separation of incisal pin if less than 2mm,
laboratory remount to be carried out for eliminating occlusal disharmony.
If the gap is more than 2mm better repeat the dentures.
Gap

## Slide 20
Point is on masticatory cusp tip :
-Deepen and widen its corresponding fossa (PLUNGER CUSP LAW) .
b. Non working side contact (Masticatory cusp) on balancing side
  Premature contact during eccentric relation if noticed on masticatory cusp –then modify the cusp .
-Repeat till the “multiple centric contact ” developed .
“Incisal pin contacts incisal guide table ”.
Correction done by selective grinding procedure
(Negative Coronoplasty)

## Slide 21
c. Eliminating high points in eccentric relation:
1). Lateral relation:
-Follow “BULLS LAW ”
– grinding occlusal inner inclines of buccal of upper & lingual of lower cusp .
- Never modify mesiopalatal cusp of maxillary second molar .
Premature incisal contact – palatal aspect of upper or labial edge/ aspect of lower incisors

## Slide 22: Finishing & polishing

## Slide 24: Thank You