AGAR REVERSIBLE HYDROCOLLOID- A REVIEW

SIDDHARTHAN¹, SANJNA NAYAR², B.RAMYA³

1. Tutor, Department of Prosthodontics, Sree Balaji Dental College & Hospital, BIHER.

2. Head of the department, Department of Prosthodontics, Sree Balaji Dental College & Hospital, BIHER.

3. CRI, Department of Prosthodontics, Sree Balaji Dental College & Hospital, BIHER.

RUNNING TITLE: AGAR REVERSIBLE HYDROCOLLOID

TYPE OF ARTICLE: REVIEW ARTICLE

CORRESPONDING AUTHOR:

Dr. Siddharthan

Tutor

Department of Prosthodontics.

Address:

Sree Balaji Dental College & Hospital,

Velachery main road,

Narayanapuram,

Pallikaranai,

Chennai- 10

EMAIL: siddharthan2896@gmail.com

Phone No: 9487124273

Source of funding: NIL

Conflict of interest: NIL

AGAR REVERSIBLE HYDROCOLLOID- A REVIEW

Siddharthan¹, Sanjna Nayar², B.Ramya³

¹Tutor, ²Head of the department, ³CRI, Department of prosthodontics,

Sree Balaji Dental College & Hospital Chennai

ABSTRACT

Agar a reversible hydrocolloid is an organic colloid derived from red seaweed. Agar was the first elastic impression material used as duplicating material and for recording crown impression. Agar requires a three sections of conditioning unit which consists of liquefaction, storage, tempering section and agar also require a special tray called water cooled rim lock trays. Agar has a good elastic property and can be reused. This article will discuss the history, composition, manipulation, disinfection, uses, merits and demerits.

INTRODUCTION

Agar- Agar is an organic colloid derived from the cell wall of red seaweed marine algae of class Rhodophyceae. A colloidal system basically consists of two phases: the dispersed phase and dispersion phase. If dispersion phase of colloidal system is water, it is called hydrocolloid. Hydrocolloid impression materials are based on the suspension of polysaccharide in water. Agar reversible hydrocolloid introduced into dental profession in 1925 by Alphons Poller as impression material. It was termed as 'Nega col' initially and later termed as "Dentacol" when introduced into dentistry. Agar was first introduced into dentistry for recording Crown impression in 1937 by Sears and was the first elastic impression material. It is essentially hydrophilic emulsoid polysaccharides. It is sulphuric ester of linear polymer of galactose1

COMPOSITION

| Materials | Functions | Percentage |
| --- | --- | --- |
| Agar | Brush heap structure | 13-17% |
| Borates | Strength; gypsum retarder | 0.2-0.5% |
| Potassium sulphates | Gypsum hardner | 1.0-2.0% |
| Wax | Filler | 0.5-1.0% |
| Thixotrophic material | Plasticizer | 0.3-0.5% |
| Water | Dispersion medium/ Reaction | 80% |
| Alkylbenzoate | Preservative | 0.1% |
| Colouring & flavoring agents |  |  |

SETTING REACTION

Agar provides a thermoreversible gel and sol gel formation is reversible and depends on temperature. The material forms a colloid after absorbing water which liquifies between 71-1000c and sets to gel again between 30- 500c. The setting of reversible hydrocolloid is called gelation. Agar is insoluble in cold water and soluble in boiling water.

MANIPULATION

This process requires a three compartment conditioning unit. Agar placed in boiling water at 1000C for 10 minutes in liquefaction section. Then it is placed in storage section at 650C to retain the sol condition until it is needed for impression. Then the tray is filled with hydrocolloid sol from the storage bath, a gauze pad is placed over the top of the tray material of the conditioning unit. The tempering time is 3- 10 minutes, just sufficient to ensure that material has reached a lower temperature. The loaded tray should never be left in this bath for more than 10 minutes as partial gelation can occur. Gelation is accelerated by circulating cool water (approx 18-200C) through the tray for 3-5 minutes. During the gelation process, the tray must be held in the mouth until gelation has proceeded to a point at which the gel strength is sufficient to resist deformation.

DISINFECTION

The hydrocolloid impression can be disinfected by nanosilver, sodium hypochlorite or glutaraldehyde as an antibacterial or antimicrobial agent for 10 mins which can be eliminate disinfecting process without sufficient dimensional Change2.

RECENT TECHNIQUE

Wet field technique

The oral soft tissues are flooded with warm water. The syringe material is then injected into the surface to be recorded. Before syringe material gels tray material is seated. The hydraulic pressure of viscous tray material forces fluid syringe material down into areas to be recorded. The motion displaces the syringe material as well as blood and debris throughout the sulcus1.

Laminate technique(agar-alginate technique)

The general procedure is to heat the agar to be placed into reusable syringes for about 6 minutes in boiling water. The agar is stored for at least 10 mins at 650c before being syringed around the preparation. A mix of alginate containing 10 percent more water than normally recommended is placed in tray and it is immediately seated over the agar syringe material. The cool mix of alginate helps gel the agar, and when the alginate has set, the combined impression is removed. The technique simplifies the use of agar and provides an impression surface that allows for preparation of stone casts acceptable for crown and bridge application1.

PROPERTIES

Dimensional stability

Dimensional accuracy was defined as the difference in dimensions between the prepared teeth and the casts when the casts were poured immediately. For the condition of accuracy (immediate pour), the hydrocolloid impression after removal were immediately immersed in 2 percent potassium sulphate solution for 10 mins before pouring the casts. For the condition of stability (one hour pour), the hydrocolloid impression were stored for 50 mins at 100 % relative humidity and at 250C. Then they were removed from the humidor and immersed in 2 percent potassium sulphate for 10 mins before pouring3.

Strength

Agar has a compressive strength of 5000- 8000 gm/cm² and tear strength of 7000 gm/cm².

Flow & Distortion

Agar is sufficiently fluid to allow detailed reproduction of hard & soft tissue.

Compatibility with gypsum

Agar impression material contains borax, which is a retarder for setting of gypsum. This can be overcome by immersing the agar impression in solution containing a gypsum accelerator or by incorporating gypsum surface hardner1.

Accuracy

Agar produces an accurate impression. The combination of agar & alginate appears to produce excellent results and detailed accuracy.

Uses

The reversible hydrocolloid is used as duplicating material, tissue conditioner, crown & bridge impression.

MERITS

Good elastic property

Re used as duplicating material

High accuracy

Non toxic

DEMERITS

Expensive equipment required

Lower than desirable tear strength

Complexity of technique

DISCUSSION

Reversible hydrocolloid agar is derived from cell wall of red seaweed. Agar is the first elastic impression material for recording crown & bridge and used as duplicating material. The material forms a colloid after absorbing water which liquifies at 1000c and sets to gel again at 450c the setting of reversible hydrocolloid is called gelation. The manipulation of agar requires a three compartment conditioning unit. Agar placed in liquefaction section at 1000c and then placed in storage section at 450c and finally in tempering unit at 450c for 2- 10 mins to reduce the temperature of agar. The hydrocolloid impression should be disinfected with antibacterial. For accuracy of hydrocolloid impression after removal were immersed in 2 percent potassium sulphate solution for 10 mins or stored in 100 % relative humidity for 50 mins.

Agar has a good compressive and tear strength compared to alginate. Agar produces detailed reproduction of hard and soft tissues.

Most alginate impression is not capable of producing finer details as much as obtained with other elastomeric impression material. Agar produces accurate impression. The combination of agar and alginate appears to produce excellent results and detailed accuracy.

CONCLUSION

The increased use of agar impression material as a result of the development of agar alginate combination technique should level off and continue at a modest level. Increased development of dustless and higher tear strength alginates should be expected.

REFERENCE

1. Sanjay Madhavan et Al /J. Pharm.Sci. & Res. Vol.7(9), 2015, 704-707

2. S. Azemat Miri, G. Mohamad Sadeghi and M. Rabiee: Journal of Research Updates in Polymer Science, 2012, 1,52-58

3. M. H. Reisbick. : Effect of Viscosity on the Accuracy and Stability of Elastic Impression Materials, may- June, vol 52 No. 3, 1973, 407-417

4. Marjorie L. Swartz, Richard D. Norman, H. William Gilmore, and Ralph W. Phillips.: studies on syneresis and imbibition in reversible hydrocolloid, J. D. Res. June, volume 36 No. 3, 1957, 472-478

5. R.G. Craig.: Review of dental impression materials, Adv  Dent Res 2(1): August, 1988, 51-64